Sodium silicate and hexametaphosphate promote the release of (oxyhydr)oxide nanoparticles from corroding iron

Benjamin F. Trueman, Javier Locsin, Evelyne Doré, Kalli Hood, and Graham A. Gagnon

Centre for Water Resources Studies,\* Department of Civil & Resource Engineering, Dalhousie University, 1360 Barrington St., Halifax, Nova Scotia, Canada B3H 4R2  
   
 \*Corresponding author  
 E-mail: [benjamin.trueman@dal.ca](mailto:benjamin.trueman@dal.ca)  
 <Tel:902.494.6070>  
 Fax: 902.494.3105

# Abstract

Sequestrants such as polyphosphate and sodium silicate are used widely to control iron precipitation in drinking water, but less is known about their impact on iron corrosion scale. Here we characterize the nanoparticulate iron (oxyhydr)oxide suspensions that result from corroding cast iron coupons in solutions containing either sodium hexametaphosphate (3 mg P L-1) or sodium silicate (100 mg SiO2 L-1). We determined the elemental composition and size distribution of these suspensions using flow field-flow fractionation with ultraviolet, multielement, and multiangle light scattering detection (FFF-UV-MALS-ICP-MS). We used light scattering data to estimate the radius of gyration, *rg*, via the Zimm model, with *r2* ranging from 0.983–0.999. Polyphosphate and sodium silicate suspensions yielded particles in two size fractions. The smaller particles had radii of gyration equaling 21–26 nm at peak 57Fe intensity, and the larger particles had radii equaling 70–91 nm. Lead associated preferentially with these particles over free hexametaphosphate, suggesting that sequestrants may interact with iron corrosion scale to yield effective transport vectors for lead in drinking water systems.

# Introduction

Polyphosphates and sodium silicates are used widely as drinking water additives, often to control aesthetic issues caused by iron from source water and pipe corrosion. These additives have been shown to decrease the colour and turbidity of iron suspensions.1–5 They reduce particle size, alter morphology, and increase stability by imparting strongly negative zeta potentials.3–6 There is also some evidence that they control iron corrosion.7,8

Less is known about the effect of polyphosphate and sodium silicate on the release of iron from iron corrosion scale. In the short term, an elevated dose of sodium silicate (100 mg SiO2 L-1) may promote colloidal iron release from corroded iron water mains,9 but little characterization of these colloids is available. The effect of polyphosphate on iron colloid release from corrosion scale is also unclear. Iron colloids are important vectors for trace element transport in drinking water systems, which is particularly relevant for controlling lead in drinking water.10–12

Here, we characterize the nanoparticulate iron released from corroding cast iron coupons in the presence of sodium hexametaphosphate—a common polyphosphate additive—and sodium silicate. We determined the concentration and size distribution of colloids (1–1000 nm) and nanoparticles (1–100 nm) using flow field-flow fractionation (FFF) with ultraviolet absorbance, multielement, and multiangle light scattering detectors. We find that both sequestrants yield stable iron nanoparticle suspensions with similar size distributions and that these colloids bind lead readily.

# Methods

## Iron suspensions

To generate each suspension, we submerged two cast iron coupons in 50 mL of solution held inside a 50 mL polypropylene tube with a polyethylene cap (coupons were 76 × 13 × 1.5 mm3 and sourced from BioSurface Technologies). Immediately before submersion, coupons were polished with 80 and then 400 grit SiC paper.

Each solution contained 35 mg NaHCO3 L-1 (5 mg C L-1, Fisher Chemical) and either sodium hexametaphosphate (3 mg P L-1, Alfa Aesar), sodium silicate (100 mg SiO2 L-1 with a NaO:SiO2 ratio of 3.22, National Silicates), or no additive (the control suspension). After preparation and mixing, solution pH was adjusted to 7.5 ± 0.2 with HNO3 or NaOH (Fisher Chemical).

Coupons were left to stagnate for 24 hours. Afterward, each suspension was mixed by gentle swirling. Suspensions were then filtered through 0.45 µm cellulose nitrate membrane filters (Whatman) using a syringe-mounted apparatus. To minimize adsorption, the first 10 mL of each aliquot was filtered to waste, and the next 20 mL was divided between two smaller polypropylene sample tubes; one for analysis by FFF-UV-MALS-ICP-MS and the other for direct quantification of the same elements by ICP-MS after acidification to pH < 2 with concentrated trace metal grade HNO3 (Fisher Chemical). To characterize partitioning of lead, we added 200 µg Pb L-1 as Pb(NO3)2 (Fisher Chemical) to filtered sodium silicate and hexametaphosphate suspensions. Lead was allowed to react for 53 minutes before analysis by FFF.

## Field-flow fractionation

Iron suspensions were fractionated using a modified version of the method described in a recent paper.11 We used an asymmetric flow FFF system (Postnova AF2000 Multiflow) with a 300 Da poly(ethersulfone) membrane and an autosampler with a 1 mL polyether ether ketone sample loop. The system was coupled sequentially to a UV absorbance detector (Shimadzu SPD-20A), a multiangle light scattering detector (Postnova PN3621), and an ICP-MS (ThermoFisher iCAP-RQ). The mobile phase for all separations was 50 mM tris (hydroxymethyl)aminomethane, adjusted to pH 7.3 with trace metal grade HCl. FFF channel effluent was mixed with internal standards (Sc, In, and Tb) in 2% HNO3 using a mixing tee.

Method parameters are summarized in Table 1. The crossflow was maintained at 2.0 mL min-1 for the first 31 minutes of each run (including the focus and transition periods); afterward it was set to decay linearly over 2 minutes to 0.1 mL min-1. The crossflow was then maintained at 0.1 mL min-1 for 10 minutes; afterward, it was set to zero for the rinse step (the final 10 minutes of the run).

Table 1: FFF run parameters.

| Parameter | Value |
| --- | --- |
| Injection volume | 0.25 (sodium silicate) and 0.5 mL (hexametaphosphate) |
| Spacer | 500 µm |
| Total run time | 53 min |
| Detector flow | 1 mL min-1 |
| Injection flow | 0.2 mL min-1 |
| Focus flow | 2.8 mL min-1 |
| Focus period | 10 min |
| Transition period | 1 min |
| Initial crossflow | 2 mL min-1 (first 31 min of each run) |
| Crossflow decay | Linear over 2 min |
| Final crossflow | 0.1 mL min-1 (10 min) |
| Rinse step | 10 min (no crossflow) |

## Inductively coupled plasma mass spectrometry

ICP-MS data were acquired using a ThermoFisher iCAP-RQ operated in kinetic energy discrimination mode with He as the collision gas. We calibrated the ICP-MS on each analysis day using multielement standards in 2% HNO3 at 25, 100, and 250 µg L-1. Standards were introduced to the nebulizer using the ICP-MS autosampler after mixing with FFF channel effluent at the mixing tee. Calibration curves yielded median *r2* values of 0.997 and 1 for 31P and 57Fe.

Quality control spikes in the same matrix (75 µg L-1) yielded median recoveries equaling 99 and 99% of 31P and 57Fe, respectively. An independently-prepared spike at 40 µg L-1 yielded a median 57Fe recovery of 96%. Detection limits were estimated using the 3 method, with calculated separately for the elution step of 5 blanks. Median instantaneous detection limits were estimated at 1.7 and 0.13 µg L-1 for 31P and 57Fe.

The deviation of the channel thickness from its nominal value of 500 µm was estimated using a method described elsewhere,13 using ferritin and bovine serum albumin as globular protein standards with diffusion coefficients taken from literature.14,15

## Transmission electron microscopy (TEM)

At least 13 TEM images were acquired to represent each iron suspension, using a JEOL 1230 instrument. Suspensions were vortexed, and then a 50 µL aliquot from each was loaded onto a 3 mm copper TEM grid (Formvar/Carbon FCF200). Images were scaled and then processed using ImageJ 1.53k16 by thresholding to differentiate particles from the background. The Feret diameter—the maximum of all transects across each perimeter—was estimated for each particle. We used a lower cutoff for particle identification of 335 nm2, which corresponds to the smallest spherical particle that the MALS detector can identify, based on manufacturer specifications (8 nm nominal radius of gyration).

## Data analysis

We analyzed and presented the data using R version 4.1.117 and a collection of contributed packages.18–21 Material necessary to reproduce the results is available on GitHub22 and functions for post-processing FFF data are available as a separate R package.23

### Peak fitting

We estimated the fraction of colloidal iron present in each of the two light scattering peaks by fitting a two-peak model to each fractogram. Each peak was represented as a skewed Gaussian and the fractogram as their sum.

### Multiangle light scattering

We estimated the radius of gyration () associated with each light scattering peak and fractogram using the Zimm model.24–26 Specifically, we solved the following equation for , the mean squared radius of gyration:

where is a constant, and are the concentration and molar mass of the analyte, respectively, is the wavelength of the incident light, is the scattering angle, is the index of refraction of the solvent, and is the Rayleigh ratio, or the scattering intensity above baseline. For environmental colloids, , , and are usually unknown, but can be estimated by regressing on . That is,

where and are the intercept and slope of the linear regression. Before fitting the model, data collected at the smallest and largest two scattering angles (7, 12, 156, and 164°) were removed due to excessive noise (Figure 1).




Figure 1: The Zimm model described the variation in light scattering over the selected range of scattering angles, with r2 values of 0.983–0.999.

# Results and discussion

Sodium silicate and hexametaphosphate suspensions yielded similar iron fractograms (Figure 2), with primary and secondary light scattering peaks. These peaks had maxima, based on 57Fe intensity, at 33.8–35 and 44.4–45.1 minutes. Iron was also present in a broad peak, eluting between approximately 15 and 30 minutes, that did not coincide with a significant light scattering signal but did adsorb UV light at 254 nm. This peak may represent iron nanoparticles that are too small to be quantified using the online MALS detector.27 In sodium hexametaphosphate suspensions, the principal 31P peak eluted at 14–14.3 minutes, which matches the peak retention of sodium hexametaphosphate in pure water (Figure S1).




Figure 2: Fractograms representing triplicate sodium silicate and hexametaphosphate suspensions and a control suspension (no sequestrant). Theoretical hydrodynamic radius was calculated at constant crossflow, based on channel geometry and flow parameters.26 Light scattering and absorbance fractograms are displayed as the raw detector responses.

The estimated radii of gyration characterizing colloids in the primary and secondary peaks ranged from 22–26 and 70–91 nm in sodium silicate suspensions, and 21–23 and 72–76 nm in hexametaphosphate suspensions (Table 2). While the maximum scattering intensities were similar between the two peaks, the second one accounted for an estimated 5%—or less—of the total iron concentration. This is explained by the much larger particle sizes represented in the secondary peak, and the dependence of scattering intensity on both colloid concentration and size.28,29

Table 2: Estimated radii of gyration and calculated geometric (equivalent spherical) diameters.

| Suspension | Replicate | Peak | Retention time (min) | Radius of gyration (nm) | Spherical equivalent geometric diameter (nm) | % total Fe |
| --- | --- | --- | --- | --- | --- | --- |
| Sodium silicate | 1 | 1 | 35.0 | 26.3 | 67.8 | 80.0 |
| - | - | 2 | 44.5 | 69.6 | 180.0 | 5.5 |
| - | 2 | 1 | 34.3 | 21.6 | 55.7 | 64.8 |
| - | - | 2 | 45.1 | 90.6 | 234.0 | 2.1 |
| - | 3 | 1 | 34.2 | 21.7 | 56.0 | 57.9 |
| - | - | 2 | 44.7 | 78.1 | 202.0 | 2.1 |
| Hexametaphosphate | 1 | 1 | 34.3 | 20.8 | 53.8 | 61.9 |
| - | - | 2 | 44.8 | 75.0 | 194.0 | 3.7 |
| - | 2 | 1 | 33.8 | 22.2 | 57.4 | 40.9 |
| - | - | 2 | 44.8 | 72.4 | 187.0 | 0.3 |
| - | 3 | 1 | 34.2 | 23.2 | 59.8 | 44.0 |
| - | - | 2 | 44.9 | 75.8 | 196.0 | 0.5 |

### Transmission electron microscopy analysis

We identified 405 and 243 particles in TEM images representing sodium silicate and hexametaphosphate suspensions, respectively, with median Feret diameters of 47 and 61 nm (Figure 3).

Since suspensions must be evaporated on a grid for TEM analysis, aggregates present in TEM images might be different from the larger particles identified by FFF-MALS. Still, there is an approximate correspondence between the equivalent spherical diameters obtained from light scattering data and the Feret distances estimated from TEM images, especially for the primary peak at a retention time of 34–35 minutes.




Figure 3: Histograms representing particles identified in TEM images of sodium silicate and hexametaphosphate-stabilized iron suspensions.

## Analyte recovery

We integrated the 31P and 57Fe signals over each fractogram—excluding the focus period—to estimate the concentrations of each analyte. Then, we compared these estimates to the concentrations determined by direct quantification. Recovery of 57Fe was 106 3.12 and 46.7 6.59% in the sodium silicate and hexametaphosphate suspensions (Table 3). While FFF recovered essentially all of the iron in sodium silicate suspensions, complexation by hexametaphosphate may have resulted in losses of iron to waste in separations of hexametaphosphate suspensions. And since recovery of P from a sodium hexametaphosphate standard was 111%, the partial P recovery from the iron oxide suspension suggests that hexametaphosphate hydrolyzed to orthophosphate or depolymerized to trimetaphosphate,30 species that readily pass through the FFF membrane to waste (Figure S1). The partial recovery of iron may be due to chelation by trimetaphosphate,31 which would also escape retention by the membrane.

Table 3: Estimated analyte recovery, by suspension type.

| Suspension | Analyte | % recovery | Standard deviation | N |
| --- | --- | --- | --- | --- |
| Sodium silicate | 57Fe | 106.0 | 3.12 | 3 |
| Hexametaphosphate | 31P | 59.9 | 11.90 | 3 |
| - | 57Fe | 46.7 | 6.59 | 3 |

## Potential of colloids for contaminant transport

Lead partitioned readily to suspended iron oxide colloids when added to the sodium silicate and hexametaphosphate suspensions (Figure 4), with variation in 57Fe explaining r2 = 99 and 93% of variation in 208Pb, respectively. The strong apparent relationship between iron and lead is consistent with much previous research documenting lead adsorption to iron (oxyhydr)oxides,32–34 and more specifically, elevated lead in iron-rich drinking water.9,10,35,36

There was little evidence, however, of lead complexation with hexametaphosphate; the primary 31P signal at a retention time of approximately 14 minutes did not co-occur with 208Pb. This suggests that lead interacts preferentially with iron oxide colloids over free hexametaphosphate. The colloids that result from iron corrosion in the presence of a sequestrant, then, may represent an effective transport vector for lead in drinking water. The preferential partitioning of lead to iron (oxyhydr)oxide colloids was reported in another recent paper, where a much larger fraction of total lead was associated with colloidal iron than colloidal dissolved organic matter, although both groups of colloids appeared to bind lead.11 Studies of natural waters have also found that lead associated preferentially with larger colloids and is strongly correlated with colloidal iron concentrations.37




Figure 4: Fractograms representing duplicate sodium silicate and hexametaphosphate suspensions; each is paired with an equivalent suspension dosed with 200 µg Pb L-1. Light scattering and absorbance fractograms are displayed as the raw detector responses.

This transport mechanism has important implications for drinking water quality: when polyphosphate or sodium silicate is added to minimize the aesthetic impacts of iron corrosion, the iron colloids that result may bind significant quantities of lead. And even if preliminary testing yields minimal evidence of lead complexation by the sequestrant itself, its interactions with iron may result in elevated lead concentrations. Corrosion control treatment tests, then, should account for the effects of iron corrosion when it is likely to occur in the distribution system.9,10,35,36,38

# Conclusion

Sodium silicate and sodium hexametaphosphate formed nanoparticulate suspensions of iron (oxyhydr)oxide in the presence of a corroding iron surface. The size distribution of the two suspensions was similar, and particle size estimates obtained from light scattering data agreed reasonably well with those determined by TEM image analysis. Lead partitioned preferentially to iron particles over free hexametaphosphate, suggesting that the particles represent an effective transport vector for lead, and possibly for other heavy metals. This highlights a risk associated with sequestrant use in drinking water treatment: sequestrants—even those that do not form complexes with lead—may generate colloids that provide an important mobile sink for lead, potentially increasing human exposure.

# Acknowledgments

This work was funded by Mitacs through the Mitacs Accelerate Program (Reference # IT23352) and NSERC through an Industrial Research Chair program (grant no. IRCPJ: 349838-16), a Postdoctoral Fellowship (E. Doré), and a postgraduate scholarship (K. Hood). We acknowledge the technical support of Heather Daurie and the Electron Microscopy Core Facility at Dalhousie University.

# References

(1) Robinson, R. B.; Minear, R. A.; Holden, J. M. Effects of Several Ions on Iron Treatment by Sodium Silicate and Hypochlorite. *Journal - American Water Works Association* **1987**, *79* (7), 116–125. https://doi.org/[10.1002/j.1551-8833.1987.tb02882.x](https://doi.org/10.1002/j.1551-8833.1987.tb02882.x).

(2) Robinson, R. B.; Reed, G. D.; Frazier, B. Iron and Manganese Sequestration Facilities Using Sodium Silicate. *Journal - American Water Works Association* **1992**, *84* (2), 77–82. https://doi.org/[10.1002/j.1551-8833.1992.tb07307.x](https://doi.org/10.1002/j.1551-8833.1992.tb07307.x).

(3) Lytle, D. A.; Snoeyink, V. L. Effect of Ortho-and Polyphosphates on the Properties of Iron Particles and Suspensions. *Journal - American Water Works Association* **2002**, *94* (10), 87–99. https://doi.org/[10.1002/j.1551-8833.2002.tb09560.x](https://doi.org/10.1002/j.1551-8833.2002.tb09560.x).

(4) Rahman, M. S.; Gagnon, G. A. Bench-Scale Evaluation of Drinking Water Treatment Parameters on Iron Particles and Water Quality. *Water Research* **2014**, *48*, 137–147. https://doi.org/[10.1016/j.watres.2013.09.018](https://doi.org/10.1016/j.watres.2013.09.018).

(5) Li, B.; Trueman, B. F.; Rahman, M. S.; Gao, Y.; Park, Y.; Gagnon, G. A. Understanding the Impacts of Sodium Silicate on Water Quality and Iron Oxide Particles. *Environmental Science: Water Research & Technology* **2019**, *5* (8), 1360–1370. https://doi.org/[10.1039/C9EW00257J](https://doi.org/10.1039/C9EW00257J).

(6) Magnuson, M. L.; Lytle, D. A.; Frietch, C. M.; Kelty, C. A. Characterization of Submicrometer Aqueous Iron(III) Colloids Formed in the Presence of Phosphate by Sedimentation Field Flow Fractionation with Multiangle Laser Light Scattering Detection. *Analytical Chemistry* **2001**, *73* (20), 4815–4820. https://doi.org/[10.1021/ac010702m](https://doi.org/10.1021/ac010702m).

(7) Lahodny-Šarc, O.; Kaštelan, L. The Influence of pH on the Inhibition of Corrosion of Iron and Mild Steel by Sodium Silicate. *Corrosion Science* **1981**, *21* (4), 265–271. https://doi.org/[10.1016/0010-938X(81)90002-0](https://doi.org/10.1016/0010-938X(81)90002-0).

(8) Koudelka, M.; Sanchez, J.; Augustyński, J. On the Nature of Surface Films Formed on Iron in Aggressive and Inhibiting Polyphosphate Solutions. *Journal of The Electrochemical Society* **1982**, *129* (6), 1186–1191. https://doi.org/[10.1149/1.2124084](https://doi.org/10.1149/1.2124084).

(9) Li, B.; Trueman, B. F.; Munoz, S.; Locsin, J. A.; Gagnon, G. A. Impact of Sodium Silicate on Lead Release and Colloid Size Distributions in Drinking Water. *Water Research* **2020**, 116709. https://doi.org/[10.1016/j.watres.2020.116709](https://doi.org/10.1016/j.watres.2020.116709).

(10) Trueman, B. F.; Gagnon, G. A. Understanding the Role of Particulate Iron in Lead Release to Drinking Water. *Environmental Science & Technology* **2016**, *50* (17), 9053–9060. https://doi.org/[10.1021/acs.est.6b01153](https://doi.org/10.1021/acs.est.6b01153).

(11) Trueman, B. F.; Anaviapik-Soucie, T.; L’Hérault, V.; Gagnon, G. A. Characterizing Colloidal Metals in Drinking Water by Field Flow Fractionation. *Environmental Science: Water Research & Technology* **2019**, *5* (12), 2202–2209. https://doi.org/[10.1039/C9EW00560A](https://doi.org/10.1039/C9EW00560A).

(12) Trueman, B. F.; Gagnon, G. A. A New Analytical Approach to Understanding Nanoscale Lead-Iron Interactions in Drinking Water Distribution Systems. *Journal of Hazardous Materials* **2016**, *311*, 151–157. https://doi.org/[10.1016/j.jhazmat.2016.03.001](https://doi.org/10.1016/j.jhazmat.2016.03.001).

(13) Litzen, Anne. Separation Speed, Retention, and Dispersion in Asymmetrical Flow Field-Flow Fractionation as Functions of Channel Dimensions and Flow Rates. *Analytical Chemistry* **1993**, *65* (4), 461–470. https://doi.org/[10.1021/ac00052a025](https://doi.org/10.1021/ac00052a025).

(14) Clough, G.; Michel, C. C. The Role of Vesicles in the Transport of Ferritin Through Frog Endothelium. *The Journal of Physiology* **1981**, *315* (1), 127–142. https://doi.org/[10.1113/jphysiol.1981.sp013737](https://doi.org/10.1113/jphysiol.1981.sp013737).

(15) Gaigalas, A. K.; Hubbard, J. B.; McCurley, M.; Woo, S. Diffusion of Bovine Serum Albumin in Aqueous Solutions. *The Journal of Physical Chemistry* **1992**, *96* (5), 2355–2359. https://doi.org/[10.1021/j100184a063](https://doi.org/10.1021/j100184a063).

(16) Schneider, C. A.; Rasband, W. S.; Eliceiri, K. W. NIH Image to ImageJ: 25 Years of Image Analysis. *Nature Methods* **2012**, *9* (7), 671–675. https://doi.org/[10.1038/nmeth.2089](https://doi.org/10.1038/nmeth.2089).

(17) R Core Team. *R: A language and environment for statistical computing*. <https://www.R-project.org/>.

(18) Wickham, H.; Averick, M.; Bryan, J.; Chang, W.; McGowan, L. D.; François, R.; Grolemund, G.; Hayes, A.; Henry, L.; Hester, J.; Kuhn, M.; Pedersen, T. L.; Miller, E.; Bache, S. M.; Müller, K.; Ooms, J.; Robinson, D.; Seidel, D. P.; Spinu, V.; Takahashi, K.; Vaughan, D.; Wilke, C.; Woo, K.; Yutani, H. Welcome to the tidyverse. *Journal of Open Source Software* **2019**, *4* (43), 1686. https://doi.org/[10.21105/joss.01686](https://doi.org/10.21105/joss.01686).

(19) Allaire, J.; Xie, Y.; McPherson, J.; Luraschi, J.; Ushey, K.; Atkins, A.; Wickham, H.; Cheng, J.; Chang, W.; Iannone, R. *Rmarkdown: Dynamic documents for r*. <https://github.com/rstudio/rmarkdown>.

(20) Xie, Y.; Allaire, J. J.; Grolemund, G. [*R Markdown: The Definitive Guide*](https://bookdown.org/yihui/rmarkdown); Chapman; Hall/CRC: Boca Raton, Florida, 2018.

(21) Xie, Y.; Dervieux, C.; Riederer, E. [*R Markdown Cookbook*](https://bookdown.org/yihui/rmarkdown-cookbook); Chapman; Hall/CRC: Boca Raton, Florida, 2020.

(22) Trueman, B. *Sodium silicate and hexametaphosphate promote the release of (oxyhydr)oxide nanoparticles from corroding iron*. <https://github.com/bentrueman/fff-mals>.

(23) Trueman, B. *fffprocessr: Process FFF-UV-MALS-ICP-MS data*. <https://github.com/bentrueman/fffprocessr>.

(24) Kammer, F. v. d.; Baborowski, M.; Friese, K. Field-Flow Fractionation Coupled to Multi-Angle Laser Light Scattering Detectors: Applicability and Analytical Benefits for the Analysis of Environmental Colloids. *Analytica Chimica Acta* **2005**, *552* (1-2), 166–174. https://doi.org/[10.1016/j.aca.2005.07.049](https://doi.org/10.1016/j.aca.2005.07.049).

(25) Wyatt, P. J. Light Scattering and the Absolute Characterization of Macromolecules. *Analytica Chimica Acta* **1993**, *272* (1), 1–40. https://doi.org/[10.1016/0003-2670(93)80373-S](https://doi.org/10.1016/0003-2670(93)80373-S).

(26) Baalousha, M.; Kammer, F. V. D.; Motelica-Heino, M.; Hilal, H. S.; Le Coustumer, P. Size Fractionation and Characterization of Natural Colloids by Flow-Field Flow Fractionation Coupled to Multi-Angle Laser Light Scattering. *Journal of Chromatography A* **2006**, *1104* (1-2), 272–281. https://doi.org/[10.1016/j.chroma.2005.11.095](https://doi.org/10.1016/j.chroma.2005.11.095).

(27) Cuss, C. W.; Grant-Weaver, I.; Shotyk, W. Af4-ICPMS with the 300 Da Membrane To Resolve Metal-Bearing “Colloids” < 1 kDa: Optimization, Fractogram Deconvolution, and Advanced Quality Control. *Analytical Chemistry* **2017**, *89* (15), 8027–8035. https://doi.org/[10.1021/acs.analchem.7b01427](https://doi.org/10.1021/acs.analchem.7b01427).

(28) Korgel, B. A.; Zanten, J. H. van; Monbouquette, H. G. Vesicle Size Distributions Measured by Flow Field-Flow Fractionation Coupled with Multiangle Light Scattering. *Biophysical Journal* **1998**, *74* (6), 3264–3272. https://doi.org/[10.1016/S0006-3495(98)78033-6](https://doi.org/10.1016/S0006-3495(98)78033-6).

(29) Baalousha, M.; V. D. Kammer, F.; Motelica-Heino, M.; Baborowski, M.; Hofmeister, C.; Le Coustumer, P. Size-Based Speciation of Natural Colloidal Particles by Flow Field Flow Fractionation, Inductively Coupled Plasma-Mass Spectroscopy, and Transmission Electron Microscopy/X-Ray Energy Dispersive Spectroscopy: Colloids−Trace Element Interaction. *Environmental Science & Technology* **2006**, *40* (7), 2156–2162. https://doi.org/[10.1021/es051498d](https://doi.org/10.1021/es051498d).

(30) Bell, R. N. Hydrolysis of Dehydrated Sodium Phosphates. *Industrial & Engineering Chemistry* **1947**, *39* (2), 136–140. https://doi.org/[10.1021/ie50446a013](https://doi.org/10.1021/ie50446a013).

(31) Rasmussen, L.; Toftlund, H. Phosphate Compounds as Iron Chelators in Animal Cell Cultures. *In Vitro Cellular & Developmental Biology* **1986**, *22* (4), 177–179. https://doi.org/[10.1007/BF02623301](https://doi.org/10.1007/BF02623301).

(32) McKenzie, R. The Adsorption of Lead and Other Heavy Metals on Oxides of Manganese and Iron. *Soil Research* **1980**, *18* (1), 61. https://doi.org/[10.1071/SR9800061](https://doi.org/10.1071/SR9800061).

(33) Xie, L.; Giammar, D. E. Chapter 13 Influence of Phosphate on Adsorption and Surface Precipitation of Lead on Iron Oxide Surfaces. In *Developments in Earth and Environmental Sciences*; Elsevier, 2007; Vol. 7, pp 349–373. https://doi.org/[10.1016/S1571-9197(07)07013-9](https://doi.org/10.1016/S1571-9197(07)07013-9).

(34) Ainsworth, C. C.; Gassman, P. L.; Pilon, J. L.; Van Der Sluys, W. G. Cobalt, Cadmium, and Lead Sorption to Hydrous Iron Oxide: Residence Time Effect. *Soil Science Society of America Journal* **1994**, *58* (6), 1615. https://doi.org/[10.2136/sssaj1994.03615995005800060005x](https://doi.org/10.2136/sssaj1994.03615995005800060005x).

(35) Trueman, B. F.; Sweet, G. A.; Harding, M. D.; Estabrook, H.; Bishop, D. P.; Gagnon, G. A. Galvanic Corrosion of Lead by Iron (Oxyhydr)Oxides: Potential Impacts on Drinking Water Quality. *Environmental Science & Technology* **2017**, *51* (12), 6812–6820. https://doi.org/[10.1021/acs.est.7b01671](https://doi.org/10.1021/acs.est.7b01671).

(36) Masters, S.; Edwards, M. Increased Lead in Water Associated with Iron Corrosion. *Environmental Engineering Science* **2015**, *32* (5), 361–369. https://doi.org/[10.1089/ees.2014.0400](https://doi.org/10.1089/ees.2014.0400).

(37) Tanguy, V.; Waeles, M.; Gigault, J.; Cabon, J.-Y.; Quentel, F.; Riso, R. D. The Removal of Colloidal Lead During Estuarine Mixing: Seasonal Variations and Importance of Iron Oxides and Humic Substances. *Marine and Freshwater Research* **2011**, *62* (4), 329. https://doi.org/[10.1071/MF10220](https://doi.org/10.1071/MF10220).

(38) Trueman, B. F.; James, W.; Shu, T.; Doré, E.; Gagnon, G. A. *Comparing Corrosion Control Treatments for Drinking Water Using a Robust Bayesian Generalized Additive Model*; preprint; Chemistry, 2022. https://doi.org/[10.26434/chemrxiv-2022-b3f72-v3](https://doi.org/10.26434/chemrxiv-2022-b3f72-v3).